## Slide 1
Semiconductor Growth: Bulk and Low dimensional system
PHY 312

## Slide 2
Sands: silicon dioxide (SiO2)
Semiconductor growth (Si)
1. Removal of ‘O’ at 1800 °C
SiO2 + 2C → Si + 2CO
Metallic grade semiconductor
~2N pure, Impurity: ~1018 cm-3
2. Refinement using chemicals
Si + 3HCl → SiHCl3 + H2
3. Heating (~ 1000 °C) under H2
SiHCl3 + H2 → Si + 3HCl
Electronic-Grade Semiconductor
>9 N pure, Impurity: ~1011 cm-3
This is still polycrystalline Si..

## Slide 3
Czochralski Growth
Seed: A single crystal of silicon
Graphite/SiO2 crucible at ~1450 °C
Seed is slowly pulled out
Both seed and crucible are rotated

## Slide 4
Czochralski Growth
Video: YouTube

## Slide 5
Bridgman Growth
Seed: A single crystal of silicon
Graphite/SiO2 crucible at ~1450 °C
The silicon is selectively melted to crystallize
Cooling
Heating
Melt
Solid
Seed
Heater coil
Temperature
Position
Lowering

## Slide 6
Silicon Ingot

## Slide 7
Identification of crystal planes
Notch Cut along {110}

## Slide 8
Silicon Ingot cutting into wafers

## Slide 9
Identification of doping
Primary
flat
(100) n-type
Secondary flat
Primary
flat
(100) p-type
Secondary flat
Primary
flat
(111) p-type
Primary
flat
(111) n-type
Secondary flat
45 °

## Slide 10
Wafer Lapping and Edge rounding:

## Slide 11
Finally, after polishing using silica and chemical treatment
Using SiO2 particle and NaOH treatment

## Slide 12
Video: YouTube

## Slide 13
Burgers vector: magnitude and direction of the lattice distortion resulting from a dislocation in a crystal lattice.
Edge dislocation
Screw dislocation
What about point dislocation?
Image: Wikipedia

## Slide 14
Molecular beam epitaxy:
Precursors:
Ga, As, In, etc

## Slide 15
Molecular beam epitaxy:

## Slide 16
Metal organic vapor phase epitaxy:
Precursors:
Trimethylindium, (CH3)3In
Trimethylgallium, (CH3)3Ga
Triethylaluminium, (CH3)3Al
Arsene (AsH3),
Phosphine (PH3),
Silane (SiH4)
Image: PhD Thesis, Subhomoy Haldar

## Slide 17
Metal organic vapor phase epitaxy:

## Slide 18
Growth of quantum well:
Cross sectional Transmission electron microscopy
Image: PhD Thesis, Subhomoy Haldar

## Slide 19
Vapor Liquid Solid Crystal growth

## Slide 20
Nanowire growth and heterostructures
70 nm
ΔEc ≈ 600 meV
InP
InP
InAs
Au
Conduction band, Ec
QD
nanowire
nanowire
M. T. Björk et al. Nano Lett 4, 1621 (2004)
Valence band, Ec

## Slide 21
Crystal phase defined Quantum Dot
InAs Zincblende
InAs Wurtzite
GaSb shell
Nanoscale Adv., 5,1890 (2023)

## Slide 22
Nanowire growth
Video: YouTube